Brand new  YELLOW LEDs.
Characteristic 3mm:                   YELLOW 
- Forward Voltage:                      1.8 - 2.1
- Forward Current (max.):         30 mA
- Lifetime:                                     100,000 Hours
- Viewing Angle:                          30 Degree
- Typical Wave Length:             590 nm
- Luminous Intensity:               3000 mcd
- Water Clear
